Kiya Propellant

Technical Overview — Prepared for Due Diligence with Lateral Frontiers

Meddy Ben Ayed  ·  Space Pickles Aerospace  ·  April 12, 2026

Overview

Kiya is a KNSB-variant solid rocket propellant developed at Space Pickles Aerospace. It is melt-cast, sorbitol-bound, and potassium nitrate oxidized — in the same family as the classic KNSB formulations documented in experimental rocketry literature, but with deliberate compositional changes that distinguish it from any published baseline. The formulation is fully mass-scalable with a consistent oxidizer-to-fuel ratio across batch sizes.

Base Formulation (per 100 g)

| Ingredient | Amount | Role |
| --- | --- | --- |
| Potassium nitrate (KNO₃) | 61 g | Primary oxidizer |
| Ammonium nitrate (NH₄NO₃) | 4 g | Secondary oxidizer |
| Sorbitol | 35 g | Fuel and binder |
| Ferric oxide, red (Fe₂O₃) | 1 g | Burn rate catalyst |
| Glycerine | 1 cc | Plasticizer |

Performance — Base Formula

The figures below are from open-air burn testing. Chamber pressure data has not yet been collected; static fire testing with instrumentation is planned as the next characterization step.

| Parameter | Value |
| --- | --- |
| Total impulse | ~110 N·s |
| Open-air burn duration (100 g) | ~14 s |
| Open-air mass burn rate | ~7.1 g/s |

Kiya-X — AP/Al Enhanced Variant

Kiya-X is a development variant of the base formula augmented with ammonium perchlorate (AP) and aluminum powder (Al). AP increases available oxidizer concentration beyond what KNO₃ and NH₄NO₃ alone provide; aluminum serves as a high-energy metallic fuel that significantly elevates flame temperature.

Formal characterization of Kiya-X is ongoing. Observations from live testing indicate:

- Burn duration approximately 2–3 s shorter per 100 g relative to the base formula (~11–12 s open-air)

- Visibly higher flame temperature and increased luminosity

- Higher thrust output relative to Kiya base

Note: Precise AP/Al mass fractions and chamber pressure data are pending. The above reflects preliminary observations from open-air testing.

Derivation from Standard KNSB

The standard KNSB formula documented by Richard Nakka consists of 65% KNO₃ and 35% sorbitol by mass. Kiya shares the same structural backbone but introduces three modifications:

- Reduced KNO₃ (61% vs. 65%) with NH₄NO₃ as a secondary oxidizer (4%). This shifts the oxygen balance and provides additional tunability over burn rate. NH₄NO₃ is not present in Nakka’s base formula.

- Glycerine plasticizer (1 cc). Improves melt viscosity and castability during processing. Not a standard KNSB ingredient.

- Fe₂O₃ catalyst (1%). Has precedent in KNSB-variant literature, though its combination with the above modifications is specific to this formulation.

Kiya is derived from KNSB and the lineage will be recognizable to anyone familiar with experimental solid propellants. It is not, however, a reproduction of any published formula.

Pending Characterization

- Static fire testing with pressure transducer — thrust curve and chamber pressure data

- Strand burn rate measurements across pressure range

- Formal AP/Al mass fraction determination and Kiya-X performance numbers

- Grain geometry evaluation (BATES vs. core-burning) for thrust profile characterization